## Slide 1: Compact Single-Turn Coupled Inductor for MHz-Range Buck Converters with Zero-Voltage Switching
Adrian Keil1, Gean Maia de Sousa2, Vincent Lorentz³, Thomas Heckel1, Marcelo Lobo Heldwein2
1 Fraunhofer Institute for Integrated Systems and Device Technology IISB, 2 Chair of High-Power Converter Systems, Technical University of Munich
3 Chair of Electronics for Electrical Energy Storage, University of Bayreuth
June 2, 2026 - O6-5-03
May 31 - June 4, 2026

## Slide 2: Table of Contents
Motivation
Introduction to the Coupled Inductor Buck Converter
  Working Principle
  Modelling using the Transformer Model
  Effects of Coupling
Inductor Design
  Potential geometries
  Influence of coupling on the flux distribution
  Air-Gap and Winding Optimization
  Design Comparison
Experimental Prototype
Conclusion

## Slide 3: Motivation
Need for 48 V to 12 V Point-of-Load converters with very high power-density
Dominated by resonant converters (mostly LLC)
  Limited range of output regulation, often fixed-ratio
Buck
  Low power-density and efficiency when hard-switched
  Solution: High frequency and soft-switching in Triangular-Current-Mode (TCM)
Challenge: Inductor design
  Air gap fringing effect
  No interleaved windings
  Core DC-bias
Solution: Planar single-turn coupled inductor
[1] EPC9174: https://epc-co.com/epc/products/evaluation-boards/epc9174
[2] EPC9143: https://epc-co.com/epc/products/evaluation-boards/epc9143
1.2 kW LLC, fs=1 MHz, η=96.3 % 1
600 W Buck, fs =500 kHz, η=95.2 % 2
copper loss

## Slide 4: Introduction – Working Principle
Negative Coupling
Positive Coupling
Same Modulation as 2ph Buck
Coupling causes change of the slopes when other leg is pulled to vin
Zero-Voltage-Switching turn-on

## Slide 5: Introduction – Effects of Coupling
Modelling the coupled inductor as an ideal transformer and two inductors
  Voltages across the two inductors become independent!
k
0
-1
1
Lout
Lm
Lself

## Slide 6: Introduction – Effects of Coupling
Modelling the coupled inductor as an ideal transformer and two inductors
  Voltages across the two inductors become independent!
k
0
-1
1
Lout
Lm
Lself

## Slide 7: Inductor Design – Potential Geometries
Investigation of 4 different designs
  (a) and (b): Coupled
  (c) and (d): Uncoupled
Design Goals:
  Pout = 1 kW
  Vin = 48 V, Vout = 12 V
    Iripple = 100 A
  fs = 1 – 3 MHz
    Lself ≈ 70 nH
(a) Double-PQ with Dual Air Gap1
(b) Four-Pole with Dual Air Gap2
(c) PQ
(d) Vertical Gap3
Additional Air Gap
[1] S. Wang et al. “PCB Winding-Based Coupled Inductor for a High-Frequency DC/DC Converter with 99% Efficiency” Mar. 2023
[2] M. Hua et al. “Ultra-thin Coupled Inductor for a GaN-Based CRM Buck Converter” Aug. 2021
[3] J. Schäfer et al. “Novel Highly Efficient/Compact Automotive PCB Winding Inductors Based on the Compensating Air-Gap Fringing Field Concept” Sep. 2020

## Slide 8: Inductor Design – Comparison between Geometries
Coupled Designs are smaller.
Four-Pole Structure performs best while having the lowest copper-loss.
(a) Double-PQ with Dual Air Gap
(b) Four-Pole with Dual Air Gap
(c) PQ
(d) Vertical Gap
PQ

## Slide 9: Inductor Design – Flux Distribution
Different Flux-Path for DC and Fundamental
Pos. Coupling: High DC-Flux but low AC
Neg. Coupling: Low DC-Flux but high AC
0 |  | 20 |  | 40 |  | 60 |  | 80 |  | 100 | 
B[mT]
Neg. Coupling DC
Neg. Coupling AC (Fundamental)
Pos. Coupling AC (Fundamental)
Pos. Coupling DC

## Slide 10: Inductor Design – Air-Gap and Winding Optimization
Current crowds in areas of large H-field
Dual Air-Gap improves field distribution
Different winding widths avoid areas of high H-field

## Slide 11: Experimental Prototype – Build
45 x 29 x 9.5 mm

## Slide 12: Experimental Prototype - Measurements
Power density: 80 kW/L (1300 W/in³)
Boxed volume: 12.4 cm³
Maximum efficiency: 96.3% at 550 W.
Soft-switching at all loads with variable frequency

## Slide 13: Experimental Prototype - Measurements
Converter | Power | Power-Density | Efficiency
Proposed Converter | 1.0 kW | 80 kW/L | 96.3 %
Cai et al.1 | 1.0 kW | 38 kW/L | 96.0 %
Ahmed et al.2 | 1.0 kW | 42 kW/L | 97.8 %
Flexpower3 | 1.3 kW | 52 kW/L | 97.0 %
EPC4 | 1.2 kW | 90 kW/L (requires ext. C) | 97.3 %
[1] Y. Cai, M. H. Ahmed, Q. Li, and F. C. Lee, “Optimal Design of Megahertz LLC Converter for 48-V Bus Converter Application” Mar. 2020
[2] M. H. Ahmed, A. Nabih, F. C. Lee, and Q. Li, “Low-Loss Integrated Inductor and Transformer Structure and Application in Regulated LLC Converter for 48-V Bus Converter” Mar. 2020
[3] FlexPower, “BMR480 series DC-DC Converters Input 45-60 V, Output up to 108.3 A / 1300 W” Mar. 2019.
[4] EPC “EPC9174 – 40 – 60 VIN, 10 – 15 V, 100 A Output 1.2 kW 1/8th Brick Reference Design Board” 2022
Power density: 80 kW/L (1300 W/in³)
Boxed volume: 12.4 cm³
Maximum efficiency: 96.3% at 550 W.
Soft-switching at all loads with variable frequency
Similar power-density and efficiency to LLC
  Promising option for real-world applications

## Slide 14: Conclusion
Transformer model provides intuitive understanding of 2-phase coupled inductors
Coupled inductor with four-pole structure allows compact core
Dual air gaps and stepped conductor widths improve current distribution
  30% reduction in copper loss
Experimental prototype: 80 kW/L (1300 W/in³) at 1 kW output and 96.3% peak efficiency
Current Research: Calorimetric core loss characterization and core optimization
Notes:   Positive Coupling is beneficial in most cases as it reduces AC flux
  Negative coupling when DC-flux matters (high-frequency materials). Reduces core size by 50% in this case.

## Slide 15
CONTACT US
Adrian Keil1, Gean Maia de Sousa2, Vincent Lorentz3, Thomas Heckel1, Marcelo Lobo Heldwein2
May 31 - June 4, 2026
1 Fraunhofer Institute for Integrated Systems and Device Technology IISB, 2 Chair of High-Power Converter Systems, Technical University of Munich
3 Chair of Electronics for Electrical Energy Storage, University of Bayreuth

## Slide 16: Current Sensing
First-Generation Board included TMR Current Sensors

## Slide 17: Introduction – Modelling using the Transformer Model
Modelling the coupled inductor as an ideal transformer and two inductors
  Voltages across the two inductors become independent!